## Slide 1: Failure of earth dams and dikes
1
Rhône river flooding (dec 2003) - Arles (France)
People living
A dike failure is always more dangerous than the flood itself
The hazard has two components:
- Natural hazard (the flood)
- Technological hazard (the dike failure)

## Slide 2: Erosion if the main cause of earth dams and dikes
2
Mechanical
Instabilities
Overflowing and surface erosion
Internal erosion

## Slide 3: Overflowing (steady overtopping) with soil erosion
3
Cohesive soil
Initiation
Development
Headcut erosion
(impinging jet)
Cohesionless soil
Initiation
Development
Missouri (2011)

## Slide 4: Irphe Small scale testing (G. Charrier PhD thesis)
4
(G. Charrier, F. Anselmet, M. Amielh, L. Pietri, 2015)
    Modified Herode Flume to study dike overflowing
    (G. Charrier PhD Thesis)
    Head-cut erosion
    The step scorrespond to the construction layers
Breach width (mm)
Time (mn)

## Slide 5: Overflowing Field tests
5
2016 Field tests
(Vidourle river)
2018 Field tests
(Rhône river)

## Slide 6: Overflowing Field tests – Example of results
6
Crest water level
Erodible soil
Resistant soil
The dike after testing
(erodible soil)
    Duration
    Flow rate
    Water level on crest
    Slope
    Vegetal cover
Time (mn)
Crest water level (cm)
Maximum erosion (cm)
    8h
    0.4 m3/s/mL
    40 cm (rate 15 cm/h)
    2.5/1
    40 cm

## Slide 7: Physics of Overflowing Erosion
7
    Skimming flow over a steep stepped slope
    (turbulent aerated flows)
Head cutting erosion

## Slide 8: Field tests – Example of results
8
    The Chanson model (1994) is used for measurement analysis
    Erosion depth
    (Lidar scanner)
    Erodible soil
    Resistant soil

## Slide 9: Impinging Jet with Erosion (Jet Erosion test)
9
kd
1
Erosion Rate (m/s)
Shear stress (Pa)
Time (s)
Scour depth (mm)

## Slide 10: Impinging Jet with Erosion (Jet Erosion test)
10
    CFD modeling with wall erosion and remeshing
    (F. Mercier PhD Thesis)
Mercier F., Bonelli S., Anselmet F. et al., J. Hydraul. Eng. ASCE, 2014
Mercier F., Bonelli S., Anselmet F. et al., Eur. J. Mech. B/Fluids, 2015
    non cohesive soil
    cohesive soils
    measurement
    measurement

## Slide 11: Pipe Flow Wih Erosion
11
    Field Test in Norway (FP5 Project, 2003)
St Julien des Landes 1969
2001 Marne/Rhin Canal

## Slide 12: Pipe flow with erosion (Hole Erosion test)
12
Erosion Rate (x10 -3 m/s)
Shear stress (Pa)

## Slide 13: Pipe flow with erosion (Hole Erosion test)
13
    CFD modeling with wall erosion and remeshing (F. Mercier PhD Thesis)
    Pressure drop (Pa)
    Time (s)
    Measurement
Mercier F., Bonelli S., Anselmet F., et al., Acta Geotechnica (2015)